Figure A.1. XRD patterns for clinkers produced in conventional (A-CC, B-CC) and high carbon dioxide (A-CC-CO2, B-CC-CO2) atmospheres.

Table A.1. Average weight loss for clinker samples exposed to conventional (A-CC, B-CC) and high carbon dioxide (A-CC-CO2, B-CC-CO2) atmospheres. The weight loss for each clinker is an average of 8–9 batches exposed in the tube furnace.

|  | A-CC | A-CC-CO2 | B-CC | B-CC-CO2 |
| --- | --- | --- | --- | --- |
| Weight loss (wt.-%) | 35.4 | 34.8 | 35.9 | 35.6 |

Table A.2. Bulk composition of all 68 elements analysed in the study, as determined by ICP-SFMS, for both raw meal and clinker samples. Concentrations given as mg/kg.

|  | A-RM | A-CC | A-CC-CO2 | B-RM | B-CC | B-CC-CO2 |
| --- | --- | --- | --- | --- | --- | --- |
| Ag | <0.1 | <0.10 | <0.10 | <0.1 | <0.10 | <0.1 |
| Al | 18400 | 28300 | 28700 | 21000 | 32200 | 33400 |
| As | 5.32 | 7.8 | 6.99 | 6.25 | 10.8 | 9.62 |
| Au | <0.05 | 0.0571 | <0.05 | <0.05 | <0.05 | <0.05 |
| B | 30.7 | 45.7 | 43.7 | 27.9 | 38.6 | 38.4 |
| Ba | 135 | 209 | 212 | 145 | 237 | 228 |
| Be | 0.949 | 1.5 | 1.36 | 0.634 | 1.66 | 1.71 |
| Bi | 0.12 | <0.05 | <0.05 | 0.108 | <0.05 | <0.05 |
| Ca | 321000 | 505000 | 480000 | 332000 | 516000 | 545000 |
| Cd | 0.383 | 0.168 | <0.05 | 0.108 | <0.05 | <0.05 |
| Ce | 26.8 | 48.2 | 47.6 | 22.2 | 36.3 | 36.2 |
| Co | <3 | 4.61 | 4.22 | 11.9 | 19.4 | 18.7 |
| Cr | 27 | 34.3 | 31.5 | 34 | 44.4 | 40.1 |
| Cs | 1.13 | <0.05 | <0.1 | 3.67 | 0.477 | 0.816 |
| Cu | 5.11 | 8.64 | 7.21 | 12.6 | 16.4 | 16.3 |
| Dy | 2.03 | 3.12 | 3.09 | 1.82 | 2.83 | 2.68 |
| Er | 1.2 | 1.99 | 1.77 | 1.03 | 1.56 | 1.56 |
| Eu | 0.497 | 0.798 | 0.777 | 0.45 | 0.708 | 0.665 |
| Fe | 13400 | 22000 | 19500 | 13000 | 22300 | 22600 |
| Ga | 3.04 | 5.02 | 5.92 | 6 | 8.42 | 9.28 |
| Gd | 2.4 | 3.38 | 3.53 | 1.79 | 3.02 | 2.96 |
| Ge | <10 | <10 | <10 | <10 | <10 | <10 |
| Hf | 1.53 | 2.6 | 2.64 | 1.15 | 1.78 | 1.67 |
| Hg | 0.223 | <0.05 | <0.05 | 0.0682 | 0.06 | <0.05 |
| Ho | 0.392 | 0.613 | 0.622 | 0.371 | 0.504 | 0.562 |
| Ir | <0.05 | <0.05 | <0.05 | <0.05 | <0.05 | <0.05 |
| K | 6980 | 1540 | 5390 | 7770 | 3910 | 7430 |
| La | 13.6 | 23.1 | 23.2 | 10.8 | 17 | 17 |
| Li | 11.8 | 15.6 | 20 | 11.9 | 15.4 | 20 |
| Lu | 0.139 | 0.209 | 0.205 | 0.144 | 0.195 | 0.176 |
| Mg | 14400 | 22600 | 22600 | 4740 | 7720 | 7860 |
| Mn | 513 | 793 | 753 | 2950 | 4470 | 5160 |
| Mo | <2 | 1.97 | 2.18 | <0.5 | <0.5 | <0.5 |
| Na | 1310 | 1500 | 1700 | 625 | 695 | 793 |
| Nb | 4.92 | 8.4 | 8.3 | 3.52 | 5.85 | 5.93 |
| Nd | 11.9 | 18.9 | 18.7 | 9.78 | 14.9 | 14.9 |
| Ni | 7.24 | 14.8 | 12.8 | 27.3 | 43.9 | 41.2 |
| P | 130 | 227 | 185 | 411 | 586 | 626 |
| Pb | 13.6 | <1 | <1 | 13.5 | 2.24 | 2.35 |
| Pd | 3.14 | 4.64 | 4.88 | 2.84 | 4.23 | 4.14 |
| Pr | 2.9 | 4.58 | 4.37 | 2.34 | 3.7 | 3.53 |
| Pt | 0.0708 | 103 | 99.2 | <0.05 | 67.3 | 72.4 |
| Rb | 27.4 | 1.84 | 11.7 | 43.8 | 11.7 | 26.9 |
| Re | <0.05 | <0.05 | <0.05 | <0.05 | <0.05 | <0.05 |
| Rh | <0.5 | <0.5 | <0.5 | <0.5 | <0.5 | <0.5 |
| Ru | <0.5 | <0.5 | <0.5 | <0.5 | <0.5 | <0.5 |
| S | 4380 | 598 | 1020 | 1120 | 232 | 310 |
| Sb | 0.23 | 0.381 | 0.339 | 0.749 | 1.06 | 1.06 |
| Sc | 3.87 | 5.91 | 5.9 | 4.38 | 7.34 | 7.21 |
| Se | 6.22 | 2.26 | 10.9 | <2 | 19.6 | 14.6 |
| Si | 67100 | 106000 | 102000 | 68200 | 110000 | 115000 |
| Sm | 2.34 | 3.66 | 3.64 | 1.92 | 3.03 | 3.04 |
| Sn | 0.934 | 1.77 | 1.74 | 0.723 | 1.14 | 1.17 |
| Sr | 216 | 345 | 344 | 215 | 340 | 342 |
| Ta | 0.235 | 0.321 | 0.301 | 0.218 | 0.312 | 0.307 |
| Tb | 0.406 | 0.629 | 0.629 | 0.338 | 0.53 | 0.536 |
| Te | <0.5 | <0.5 | <0.5 | <0.5 | <0.5 | <0.5 |
| Th | 6.26 | 10.4 | 10.1 | 3.23 | 4.9 | 4.89 |
| Ti | 1530 | 2340 | 2420 | 1030 | 1580 | 1660 |
| Tl | 3.62 | <0.05 | <0.05 | 2.21 | <0.05 | <0.05 |
| Tm | 0.148 | 0.234 | 0.221 | 0.154 | 0.198 | 0.208 |
| U | 2.16 | 3.61 | 3.44 | 0.968 | 1.49 | 1.52 |
| V | 64.7 | 104 | 97.7 | 35.3 | 50.4 | 46.6 |
| W | <1 | <1 | <1 | <1 | 1.14 | <1 |
| Y | 11.7 | 20 | 20 | 10.8 | 17.2 | 17.3 |
| Yb | 1.06 | 1.7 | 1.64 | 0.945 | 1.44 | 1.48 |
| Zn | 379 | 597 | 528 | 23.1 | 35.6 | 29.8 |
| Zr | 53.8 | 87.8 | 96.5 | 39.6 | 59.1 | 58.8 |