# Appendix A

Supplementary data

# Influence of Jaw Angle in Smart Crushing on Selective Recovery of Recycled concrete fines

Winnie Franco Santos1 , Sonal Deo1, Jos Brouwers1

1Department of the Built Environment, Eindhoven University of Technology, P.O. Box 513, 5600 MB Eindhoven, the Netherlands

Corresponding author: w.franco.santos@tue.nl

Table S1 -XRD corresponding 1 ơ errors values on the pattern fit and criteria of fit to evaluate the quality of Rietveld refinement.

CEM I angle 1 (0-63 µm)

| Phase Name | ơ errors |  | Criteria of fit | Value |
| --- | --- | --- | --- | --- |
| Quartz low | 0.841 |  | GOF | 2.18 |
| Serpentine | 0.156 |  | Rexp | 4.06 |
| Phlogopite | 0.293 |  | Rwp | 8.85 |
| Calcite | 0.351 |  | Rp | 6.47 |
| Silicon | 0 |  | Rexp' | 6.18 |
| Gypsum | 0.145 |  | Rwp' | 13.49 |
| Portlandite | 0 |  | Rp' | 10.47 |
| Anorthite | 0 |  | Weighted Durbin Watson | 0.5 |
| Anorthoclase | 0 |  |
| Albite | 0.184 |  |
| Aragonite | 0 |  |
| Vaterite | 0.128 |  |
| Ettringite | 0.327 |  |
| Portlandite | 0.162 |  |
| Amorphous | 1.348 |  |

CEM I angle 2 (0-63 µm)

| Phase Name | ơ errors |  | Criteria of fit | Value |
| --- | --- | --- | --- | --- |
| Quartz low | 0.865 |  | GOF | 2.27 |
| Serpentine | 0.65 |  | Rexp | 4.07 |
| Phlogopite | 0.356 |  | Rwp | 9.21 |
| Calcite | 0.472 |  | Rp | 6.83 |
| Silicon | 0 |  | Rexp' | 6.14 |
| Gypsum | 0.119 |  | Rwp' | 13.91 |
| Portlandite | 0 |  | Rp' | 10.94 |
| Anorthite | 0 |  | Weighted Durbin Watson | 0.46 |
| Anorthoclase | 0 |  |
| Albite | 0.209 |  |
| Aragonite | 0 |  |
| Vaterite | 0.142 |  |
| Ettringite | 0.334 |  |
| Portlandite | 0.136 |  |
| Amorphous | 1.599 |  |

CEM III angle 1 (0-63 µm)

| Phase Name | ơ errors |  | Criteria of fit | Value |
| --- | --- | --- | --- | --- |
| Quartz low | 0.553 |  | GOF | 1.72 |
| Serpentine | 0.124 |  | Rexp | 4.18 |
| Phlogopite | 0.282 |  | Rwp | 7.19 |
| Calcite | 0.362 |  | Rp | 5.66 |
| Silicon | 0 |  | Rexp' | 6.45 |
| Gypsum | 0.132 |  | Rwp' | 11.1 |
| Portlandite | 0 |  | Rp' | 9.24 |
| Anorthite | 0 |  | Weighted Durbin Watson | 0.78 |
| Anorthoclase | 0.289 |  |
| Albite | 0.254 |  |
| Aragonite | 0 |  |
| Vaterite | 0.196 |  |
| Ettringite | 0.254 |  |
| Portlandite | 0.103 |  |
| Amorphous | 1.161 |  |

CEM III angle 2 (0-63 µm)

| Phase Name | ơ errors |  | Criteria of fit | Value |
| --- | --- | --- | --- | --- |
| Quartz low | 0.729 |  | GOF | 2.13 |
| Serpentine | 0.137 |  | Rexp | 4.13 |
| Phlogopite | 0.354 |  | Rwp | 8.78 |
| Calcite | 0.364 |  | Rp | 6.7 |
| Silicon | 0 |  | Rexp' | 5.9 |
| Gypsum | 0.089 |  | Rwp' | 12.55 |
| Portlandite | 0 |  | Rp' | 10.04 |
| Anorthite | 0 |  | Weighted Durbin Watson | 0.54 |
| Anorthoclase | 0.689 |  |
| Albite | 0.295 |  |
| Aragonite | 0 |  |
| Vaterite | 0.199 |  |
| Ettringite | 0.281 |  |
| Portlandite | 0.124 |  |
| Amorphous | 1.511 |  |