Supporting Information

Single layer woven carbon fibers improved the thermal and mechanical properties of epoxy resin

A Romo-Uribe & A Reyes-Mayer

| Figure S1. (a) Shear viscosity as a function of shear rate, at the indicated temperatures of EPON 828 epoxy resin. (b) Shear viscosity as a function of temperature. The dotted line corresponds to an exponential fit to the data ηo=118.98e-0.108T. |  |
| --- | --- |

| Figure S2. FTIR spectra of (a) EPON 828, and (b) 4,4’-diamino diphenylmethane (DDM). |  |
| --- | --- |
| Figure S3. FTIR spectrum of crosslinked EPON 828 with DDM at 80°C for 180 min. |  |

Figure S4. DSC heating traces of Epon 828 crosslinked with DDM for the time indicated in each plot and at (a) 110°C, (b) 130°C, and (c) 150°C. Endothermic heat is upward.

Figure S5. Stress-strain traces of Epon 828 crosslinked with DDM at (a) 80°C, (b) 100°C, (c) 110°C, (d) 130°C and (e) 150°C. Uniaxial tensile tests were carried out at room temperature, straining at 5 mm/min and fresh specimens were used for each test.

Table S1. Band identification of reagents EPON 828 and 4,4’-diamino diphenylmethane (DDM).

| Reactive | Functional groups | Wavenumber (cm-1) | Description | Reference |
| --- | --- | --- | --- | --- |
| EPON 828 |  |  |  |  |
|  | -OH stretching Stretching of C-H of the oxirane ring vC-H aromatic vC-H of the epoxy StretchingC-H of CH2 and CH aromatic and aliphatic vC-H aliphatic C=O stretching of esters Stretching C=C of aromatic rings vC=C of the 1-4-substituted benzene Stretching C-C of aromatic CH2 (scissoring) / symCH3 + vC=C of the 1-4-substituted benzene CH2t (twisting of the epoxy group) C-H benzenic Stretching C-O-C of ethers C-H of the 1-4-substituted benzene + vsymC-O-C in the case of an aromatic ether Stretching C-O of oxirane group Characteristic vibration of the epoxide ring corresponding to vasym Stretching C-O-C of oxirane group γC-H of the 1-4-substituted benzene + γCH2r of the epoxide group Rocking CH2 γCH2r (rocking)+ γC-H of the dissubstituted benzene; 1-4-substituted benzene (four adjacent hydrogens) | 3500 3057 3058, 3038 3000 2965- 2873 2969, 2930, 2873 1730 1608 1608, 1582, 1508 1509 1458 1347 1184, 1155 and 1085 1036 1036 915 915 831 831 772 770-760 | The broad band at 3500 cm-1 is assigned to O-H stretching of hydroxyl groups, revealing the presence of dimers or high molecular weight species. C-H stretching of terminal oxirane group is observed at 3057 cm-1 and is attributed to the C-H tension of the methylene group of the epoxy ring. The main features observed in the spectrum are only the overtones of C-H and CH2 stretching bands. The bands corresponding to the stretching of esters. There are also bands corresponding to the ether linkage located at 1000-1100cm-1. Apart from the oxirane absorptions this resin shows the bands corresponding to the stretching C-O-C of ethers (1100 cm-1). C-O deformation band is centered at 915 cm-1 in DGEBA also is attributed to the C-O deformation of the oxirane group. | [1] [2] [1] [2] [1] [2] [1] [2] [1] [2] [1] [2] [1] [2] [1] [2] |
| DDM | NH2 asymmetric stretch NH2 symmetric stretch Ring-CH symmetric stretch Ring-CH asymmetric stretch CH2 asymmetric stretch CH2 symmetric stretch NH2 deformation + ring deformation NH2 deformation, ring deformation + NH2 deformation Ring deformation Ring-CH ip-bend, Ring-CH ip-bend + CCC asymmetric stretch CH2 scissor Ring deformation + CH2 scissor Ring deformation + CH2 rock Ring CH deformation Ring-H bend + CH2 rock + NH2 rock, ring deformation + CH2 twist Ring deformation + CH2 rock C–N symmetric stretch + ring deformation CH2 wag + CCC asymmetric stretch CCC asymmetric stretch, Ring-CH asymmetric ip-bend + CH2 twist Ring-CH symmetric ip-bend, CH2 twist + ring-CH asymmetric ip-bend Ring-CH asymmetric ip-bend + NH2 wag NH2 wag + ring deformation Ring deformation Ring-CH wag Ring-CH wag, CH2 rock + ring-CH deformation Ring-CH deformation + CH2 rock Rink breathing + ring-CH deformation Ring-CH wag CCC asymmetric stretch Ring-CH wag Ring deformation | 3441, 3414 3336, 3317 3212 3208, 3057, 3032, 3015, 2899 2885 2826 1629 1611 1581 1515 1459 1433 1425 1334 1324 1316 1288 1275 1207 1176 1150, 1126 1080 1013 961, 951 951 909 843 819, 811 781 765 709, 648, 630 | The most intense bands in the region above 3100 cm-1 in the infrared spectra of MDA is assigned to the NH2 stretching vibrations. The assignments of the ring-CH, CH2 and CH3 stretching modes The 1629 cm-1 band and the 1618 cm-1 line in the spectra of the MDA are due to ring and NH2 deformations, The 1611 cm-1 band and 1618 cm-1 line in the spectra of the ring-CH bending mode and ring bending deformation, respectively. The 1516 cm-1 band is a ring-CH bending mode. | [3] [3] |
| DGEBA-DDM | OH stretch NH2 asymmetric, and stretch, respectively Epoxy CH2 asymmetric, and phenyl CH stretch Phenyl CH stretch Epoxy CH2 symmetric CH3 asymmetric, stretch CH2 asymmetric, stretch CH3 asymmetric, stretch and CH stretch CH2 symmetric, stretch CH2 Epoxy deformation | 3550, 3409 3460, 3370 3054 3034 2997 2969 2930 2871 2840 1460 916 | Can be assigned to the vibration of OH groups. Can be assigned to the vibration of NH2 groups. The overlapped peaks from 3100 to 2800 cm_1 are assigned to the CH/CH2/CH3 vibrations of epoxy groups, benzene groups, and backbone. | [4] [4,5] [4] [5] [4] |

References

- González, M. G., Cabanelas, J. C., & Baselga, J. (2012). Applications of FTIR on Epoxy Resins - Identification, Monitoring the Curing Process, Phase Separation and Water Uptake. Infrared Spectroscopy - Materials Science, Engineering and Technology. doi:10.5772/36323. Chap 13

- Cherdoud-Chihani, A., Mouzali, M., & Abadie, M. J. M. (1998). Study of crosslinking AMS/DGEBA system by FTIR. Journal of Applied Polymer Science, 69(6), 1167–1178. doi:10.1002/(sici)1097-4628(19980808)69:6<1167::aid-app14>3.0.co;2-q

- H. M. (2013). A comparative study of the structure and vibrational spectra of diphenylmethane, the carcinogen 4,4′-methylenedianiline and 4,4′-methylenebis(N,N-dimethylaniline). Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 109, 213–220. doi:10.1016/j.saa.2013.02.030

- Li, L., Wu, Q., Li, S., & Wu, P. (2008). Study of the Infrared Spectral Features of an Epoxy Curing Mechanism. Applied Spectroscopy, 62(10), 1129–1136. doi:10.1366/000370208786049204

- Varley, R. J., Heath, G. R., Hawthorne, D. G., Hodgkin, J. H., & Simon, G. P. (1995). Toughening of a trifunctional epoxy system: 1. Near infra-red spectroscopy study of homopolymer cure. Polymer, 36(7), 1347–1355. doi:10.1016/0032-3861(95)95911-j