Supporting Information for

## Modelling the piping-assisted erosion of clay barriers

Huaxiang Yan1,2, Majid Sedighi2*, Andrey Jivkov2, Abdelmalek Bouazza3

1 MOE Key Laboratory of Soft Soils and Geoenvironmental Engineering, Zhejiang University, Hangzhou 310058, China

2 Department of Mechanical, Aerospace and Civil Engineering, School of Engineering, The University of Manchester, Manchester, M13 9PL, UK

3 Department of Civil Engineering, Monash University, 23 College Walk, Melbourne, VIC 3800

* Corresponding author: majid.sedighi@manchester.ac.uk

This supporting information file has 4 pages, including

2 Texts: Text S1, Test S2

1 Figures: Figure S1

6 References

Text S1

Figure S1 presents the modelling result of the solid volume fraction of bentonite with time across the width of the sample for rh= 3 mm (Fig. S1a) and rh= 6 mm (Fig. S1b) piping channel. It can be observed that there is almost no bentonite expanding into the piping channel, as the swelling velocity is much smaller than the erosion rate. The water velocities (Vl) for rh=3 mm and rh=6 mm are 0.06 m/s and 0.015 m/s, respectively (Sane et al., 2013). The maximum expansion diffusivity of bentonite colloid (DR) is 10-9 m/s (Nerenieks et al., 2009; Yan et al., 2021). The dimensionless Peclet number (Pe=VlL/DR) is used to identify the impacts of expansion rate and flow rate on the overall process. The Peclet numbers for rh=3 mm and rh =6 mm are 6106 and 1.5106, respectively, demonstrating that the erosion rate induced by the water flow can be significantly larger than that of the expansion rate. It is noted that the flowing water continually eroded the bentonite mass that was separated from the sample and released into the piping channel. The solid fraction profile decreased as time increased (Fig. S1). For example, the solid fraction of bentonite decreased from 59% to 32 % at r=40 mm during 40 hours of water-clay interaction (t=10 h to t=50 h, Fig. S1).

Figure S1

(a)

(b)

Figure S1. Modelling results of the solid volume fraction of bentonite with time (a) rh =3 mm piping channel and (b) rh =6 mm piping channel

Test S2

The separation distance between the flat particles (h) is directly controlled by the solid fraction of clay and can be described by (Laxton and Berg, 2006)

| h=δpϕsmaxϕs-1 | (S-1) |
| --- | --- |

where ϕsmax is the maximum clay solid volume fraction.

The expression of attractive van der Waals forces (FA) and repulsive electrical double layer forces (FR) is given by

| FA=AHSp6π1h3-2h+δp3+1h+2δp3 | (S-2) |
| --- | --- |
| FR=2cRTSpcoshym-1 | (S-3) |

where AH is the Hamaker constant, Sp is the surface area of the particles, the function ym represents the scaled potential in the midpoint between parallel plates. The function ym represents the non-dimensional potential in the midpoint between parallel plates of, for example, a fracture, described by Liu et al. (2009) and Sedighi et al. (2021):

| ym=sinh-12sinhy∞m+4κhsinhy∞h2 | (S-4) |
| --- | --- |

where

| y∞m=4tanh-12tanh0.5sinh-1zFσ02ε0εRRTκexp-κh2 | (S-5) |
| --- | --- |
| y∞h=4tanh-1tanh0.5sinh-1zFσ02ε0εRRTκexp-κh | (S-6) |

The Debye length (κ) is given by:

| κ=2cz2F2ε0εRRT | (S-7) |
| --- | --- |

where F is the Faraday’s constant; z is valence of ions in the mid-plane and ε0εR is the dielectric constant.

References

Laxton, P.B. and Berg, J.C., 2006. Relating clay yield stress to colloidal parameters. Journal of colloid and interface science, 296(2), 749-755.

Liu, L., Moreno, L. and Neretnieks, I., 2009. A dynamic force balance model for colloidal expansion and its DLVO-based application. Langmuir, 25(2), 679-687.

Neretnieks, I., Longcheng, L. and Moreno, L., 2009. Mechanisms and models for bentonite erosion (No. SKB-TR--09-35). Swedish Nuclear Fuel and Waste Management Co.

Sane, P., Laurila, T., Olin, M. and Koskinen, K., 2013. Current status of mechanical erosion studies of bentonite buffer (No. POSIVA--12-45). Posiva Oy.

Sedighi, M., Yan, H. and Jivkov, A.P., 2021. Peridynamic modelling of clay erosion. Géotechnique, 72(6), 510-521.

Yan, H., Sedighi, M. and Jivkov, A.P., 2021. Modelling the effects of water chemistry and flowrate on clay erosion. Engineering Geology, 294, 106409.