Supplementary information of “Two-dimensional experimental assessment of interaction energy-induced suffusion in sand-clay mixtures”

Jongmuk Won1,*, and Incheol Joo1

1Department of Civil and Environmental Engineering, University of Ulsan, Daehak-ro 93, Nam-gu, Ulsan 680-749, South Korea

Contents of this file

This Supplementary information include 6 Figures and 1 Table.

Fig. S1. Pictures of sand with calculated roundness of individual sand grains used in the experiments

Fig. S2. XRD patterns of (a) kaolinite, (b) illite, and (c) bentonite used in this study (analyzed by the Korea Basic Science Institute)

Fig. S3. Median-to-mean particle size ratios at three outlets (clay content = 3%).

Fig. S4. Median-to-mean particle size ratios in the flow cell after injection (clay content = 3%).

Table S1. X-ray fluorescence (XRF) results of the sand and clay used in this study (analyzed by the Korea Basic Science Institute).

| Component | Mass percentage (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | K3 | K4 | K5 | Kaolinite | Illite | Bentonite |
| SiO2 | 82.6 | 79.9 | 74.6 | 51.6 | 60.7 | 50.8 |
| Al2O3 | 3.06 | 9.44 | 10.9 | 33.8 | 20.2 | 15.7 |
| CaO | 9.32 | 0.679 | 0.779 | 9.16 | 0.175 | 3.14 |
| Fe2O3 | 0.758 | 1.65 | 1.79 | 2.81 | 9.35 | 22.1 |
| K2O | 1.70 | 5.898 | 9.27 | 0.855 | 6.97 | 0.247 |
| Na2O | 0.044 | 1.44 | 1.73 | 0.85 | 0.471 | 1.94 |
| MgO | 1.74 | 0.128 | 0.05 | 0.38 | 0.572 | 2.60 |
| TiO2 | 0.248 | 0.148 | 0.072 | 0.285 | 1.11 | 1.45 |
| P2O5 | 0.239 | 0.214 | 0.224 | 0.114 | 0.159 | 0.476 |
| SrO | - | 0.015 | - | 0.09 | 0.017 | 0.064 |
| MnO | - | 0.097 | 0.167 | 0.026 | 0.129 | 0.084 |
| CuO | 0.029 | - | 0.022 | 0.02 | - | 0.055 |
| Cr2O3 | 0.09 | 0.109 | 0.08 | - | - | - |
| SO3 | - | 0.062 | 0.053 | - | - | - |
| Rb2O | 0.01 | 0.086 | 0.175 | - | - | - |
| ZrO2 | 0.161 | 0.037 | 0.019 | - | - | - |
| WO3 | 0.049 | 0.075 | - | - | - | - |
| PbO | - | 0.016 | 0.03 | - | - | - |
| SrO | - | 0.015 | 0.019 | - | - | - |
| Ga2O3 | - | 0.008 | 0.014 | - | - | - |
| Nb2O5 | - | - | 0.01 | - | - | - |
| ZnO | - | 0.042 | 0.049 | 0.011 | 0.020 | 0.056 |