Table SI.I

| Topology | Array | Cell size [mm] | Volume Fraction [%] | D&S | Nozzle diameter [mm] | Notes |
| --- | --- | --- | --- | --- | --- | --- |
| Body-Centred Cubic (BBC) | 1x1x1 | 15 | 10 |  | 0.6 | - Smallest beam dimension » 1 mm - Printed with and without a PVA brim |
| Simple Cubic (SC) | 2x2x3 | 7 | 40 | x | 0.4 | - Smallest beam dimension » 3 mm |
| Simple Cubic (SC) | 3x3x4 | 5 | 25 | x | 0.4 | - Smallest beam dimension » 1.6 mm |
| Matrix-based Primitive (P) | 2x3x5 | 5 | 30 | x | 0.4 | - Smallest thickness » 0.85 ¸ 0.7 mm - Created as a 20x30x50 mm3 and then scaled by 50% inside Cura) |
| Network-based IWP (IWP) | 3x3x5 | 7 | 30 | x | 0.4 | - Smallest thickness » 0.75 mm |
| Matrix-based Gyroid (MG) | 1x1x1 | 15 | 20 |  | 0.6 | - Smallest thickness » 1.5 mm - Printed with PVA as support material |
| Network-based Gyroid (G) | 1x1x1 | 15 | 25 |  | 0.6 | - Lateral walls were added (side skin 0.8mm thickness) - Printed with and without a PVA brim |
| Network-based Gyroid (G) | 1x1x1 | 12 | 50 | x | 0.6 | - Created as a 12x12x12 mm3 and with a side skin of 1.2 mm |
| Network-based Gyroid (G) | 1x1x1 | 12 | 20 | x | 0.6 | - Created as a 12x12x12 mm3 and with a side skin of 1.2 mm |
| Network-based Gyroid (G) | 2x2x2 | 8 | 50 | x | 0.6 | - Created as a 16x16x16 mm3 and with a side skin of 0.8 mm |
| Network-based Gyroid (G) | 1x1x2 | 12 | Graded (50-20) | x | 0.6 | - Graded and linear material distribution: from 50% at the bottom to 20% at the top - Created as a 12x12x24 mm3 and with a side skin of 1.2 mm |