Supplementary Material

Figure VIII. ANN with one hidden layer between an input layer and an output layer, based on (Wenzel et al. 2022)

Source: Authors’ own work

Table IV. Parameters used for the random forest regression

| Number of Measurements | Test Split | MSE | R2 |
| --- | --- | --- | --- |
| 140 | 0.2 | 1.78 units | 0.91 |

Source: Authors’ own work

Table V. Lower and upper bounds of input parameters for published red laser data

| i | Input Parameter Xi | Lower Bound LB | Upper Bound UB |
| --- | --- | --- | --- |
| 1 | Laser power | 100 W | 1200 W |
| 2 | Scanning speed | 50 mms | 1200 mms |
| 3 | Hatch distance | 10 µm | 120 µm |
| 4 | Laser spot diameter | 20 µm | 100 µm |
| 5 | Layer thickness | 10 µm | 55 µm |
| 6 | Powder size | 15 µm | 50 µm |

Source: Authors’ own work

Table VI. Lower and upper bounds of input parameters (green laser)

| i | Input Parameter Xi | Lower Bound LB | Upper Bound UB |
| --- | --- | --- | --- |
| 1 | Laser power | 100 W | 200 W |
| 2 | Scanning speed | 50 mms | 1200 mms |
| 3 | Hatch distance | 30 µm | 70 µm |
| 4 | Laser spot diameter | 40 µm | 80 µm |
| 5 | Layer thickness | 20 µm | 40 µm |
| 6 | Powder size | 20 µm | 30 µm |

Source: Authors’ own work

Table VII. Examples of unnormalized and normalized data

| Unnormalized Data | Normalized Data |
| --- | --- |
| 70 % | 0 |
| 75 % | 0.051 |
| 95 % | 0.478 |
| 99 % | 0.798 |
| 99.9 % | 0.972 |
| 100 % | 1 |

Source: Authors’ own work

Table VIII. Averaged MSE and RMSE of relative density in percentage points (red laser)

| Method | MSE | RMSE | MSE* | RMSE* |
| --- | --- | --- | --- | --- |
| PINN | 4.58 | 2.14 | 3.36 | 1.83 |
| ANN | 14.84 | 3.85 | 9.79 | 3.13 |
| Linear regression | 18.47 | 4.30 | 12.95 | 3.59 |
| *Elimination of number 11 as a potential outlier |  |  |  |  |

Source: Authors’ own work

Table IX. Averaged MSE and RMSE of relative density in percentage points (green laser)

| Method | MSE | RMSE |
| --- | --- | --- |
| PINN | 2.12 | 1.46 |
| ANN | 4.79 | 2.19 |
| Linear regression | 3.24 | 1.80 |
| Source: Authors’ own work |  |  |

Table X. Published research used for Figure I

| Number | DOI | Reference |
| --- | --- | --- |
| 1 | - | (Binghau Lu 2020) |
| 2 | 10.1007/s00501-021-01107-0 | (Bonesso et al. 2021) |
| 3 | 10.1108/RPJ-06-2018-0143 | (Guan et al. 2019) |
| 4 | 10.1007/s11837-017-2695-x | (Ikeshoji et al. 2018) |
| 5 | 10.1016/j.jmatprotec.2019.02.022 | (Jadhav et al. 2019) |
| 6 | 10.1016/j.addma.2020.101607 | (Jadhav et al. 2020a) |
| 7 | 10.1016/j.addma.2021.101990 | (Jadhav et al. 2021) |
| 8 | 10.1002/mdp2.94 | (Jadhav et al. 2020b) |
| 9 | 10.1016/j.jallcom.2022.167425 | (Jeyaprakash et al. 2023) |
| 10 | 10.1016/j.matdes.2019.108406 | (Ma et al. 2020) |
| 11 | 10.1016/j.cirp.2021.03.006 | (Overmeyer et al. 2021) |
| 12 | 10.1016/j.addma.2021.102417 | (Qu et al. 2021) |
| 13 | 10.1016/j.matlet.2021.131141 | (Shen et al. 2022) |
| 14 | 10.1016/j.addma.2019.100831 | (Silbernagel et al. 2019) |
| 15 | 10.1016/j.jallcom.2022.166627 | (Tang et al. 2022a) |
| 16 | 10.1016/j.matdes.2022.111419 | (Tang et al. 2022b) |
| 17 | 10.1016/j.addma.2021.102562 | (Tertuliano et al. 2022) |
| 18 | 10.1080/02670836.2019.1600840 | (Tiberto et al. 2019) |
| 19 | - | (Trevisan et al. 2017) |
| 20 | 10.1016/j.msea.2020.139615 | (Yan et al. 2020) |
| 21 | 10.1016/j.jallcom.2021.160475 | (Yu et al. 2021) |

Source: Authors’ own work / literature research conducted by the authors

Table XI. Research used for the extraction of data for the red laser PINN

| Number of Measurements | Reference |
| --- | --- |
| 48 (1-48) | (Bonesso et al. 2021) |
| 24 (49-72) | (Jadhav et al. 2021) |
| 17 (73-89) | (Binghau Lu 2020) |
| 17 (90-106) | (Yan et al. 2020) |
| 15 (107-121) | (Imai et al. 2020) |
| 14 (122-135) | (Qu et al. 2021) |
| 9 (136-144) | (Guan et al. 2019) |
| 6 (145-150) | (Ikeshoji et al. 2018) |
| 6 (150-156) | (Tertuliano et al. 2022) |
| 4 (157-160) | (Jadhav et al. 2019) |

Source: Authors’ own work / literature research conducted by the authors

Table XII. Data extracted from the literature in Table XI for red laser LPBF systems

| # | Laser Power [W] | Scanning Speed [mms] | Hatch Distance [µm] | Laser Spot Diameter [µm] | Layer Thickness [µm] | Powder Size [µm] | Relative Density [%] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 370 | 400 | 110 | 82 | 20 | 19.5 | 97.40 |
| 2 | 370 | 200 | 80 | 82 | 20 | 19.5 | 96.80 |
| 3 | 370 | 200 | 90 | 82 | 20 | 19.5 | 96.50 |
| 4 | 370 | 200 | 100 | 82 | 20 | 19.5 | 96.30 |
| 5 | 370 | 500 | 80 | 82 | 20 | 19.5 | 96.80 |
| 6 | 370 | 300 | 110 | 82 | 20 | 19.5 | 97.00 |
| 7 | 370 | 500 | 90 | 82 | 20 | 19.5 | 97.20 |
| 8 | 370 | 500 | 100 | 82 | 20 | 19.5 | 98.00 |
| 9 | 370 | 500 | 110 | 82 | 20 | 19.5 | 97.20 |
| 10 | 370 | 200 | 80 | 82 | 20 | 27.4 | 92.10 |
| 11 | 370 | 200 | 90 | 82 | 20 | 27.4 | 92.50 |
| 12 | 370 | 200 | 100 | 82 | 20 | 27.4 | 93.20 |
| 13 | 370 | 300 | 80 | 82 | 20 | 27.4 | 91.50 |
| 14 | 370 | 300 | 90 | 82 | 20 | 27.4 | 92.20 |
| 15 | 370 | 300 | 100 | 82 | 20 | 27.4 | 93.40 |
| 16 | 370 | 400 | 110 | 82 | 20 | 27.4 | 92.50 |
| 17 | 370 | 500 | 80 | 82 | 20 | 27.4 | 92.50 |
| 18 | 370 | 500 | 90 | 82 | 20 | 27.4 | 92.40 |
| 19 | 370 | 500 | 100 | 82 | 20 | 27.4 | 91.90 |
| 20 | 370 | 500 | 110 | 82 | 20 | 27.4 | 92.00 |
| 21 | 370 | 200 | 80 | 82 | 20 | 18.7 | 93.40 |
| 22 | 370 | 200 | 90 | 82 | 20 | 18.7 | 93.30 |
| 23 | 370 | 200 | 10 | 82 | 20 | 18.7 | 92.70 |
| 24 | 370 | 200 | 110 | 82 | 20 | 18.7 | 94.10 |
| 25 | 370 | 300 | 110 | 82 | 20 | 18.7 | 93.90 |
| 26 | 370 | 400 | 80 | 82 | 20 | 18.7 | 93.60 |
| 27 | 370 | 400 | 90 | 82 | 20 | 18.7 | 94.00 |
| 28 | 370 | 400 | 100 | 82 | 20 | 18.7 | 94.00 |
| 29 | 370 | 400 | 110 | 82 | 20 | 18.7 | 93.20 |
| 30 | 370 | 500 | 80 | 82 | 20 | 18.7 | 93.70 |
| 31 | 370 | 500 | 90 | 82 | 20 | 18.7 | 93.20 |
| 32 | 370 | 500 | 100 | 82 | 20 | 18.7 | 96.60 |
| 33 | 370 | 500 | 110 | 82 | 20 | 18.7 | 97.60 |
| 34 | 370 | 200 | 110 | 82 | 20 | 19.5 | 96.40 |
| 35 | 370 | 300 | 80 | 82 | 20 | 19.5 | 97.60 |
| 36 | 370 | 300 | 90 | 82 | 20 | 19.5 | 96.40 |
| 37 | 370 | 300 | 100 | 82 | 20 | 19.5 | 97.40 |
| 38 | 370 | 400 | 80 | 82 | 20 | 19.5 | 97.20 |
| 39 | 370 | 300 | 110 | 82 | 20 | 27.4 | 92.50 |
| 40 | 370 | 400 | 80 | 82 | 20 | 27.4 | 92.50 |
| 41 | 370 | 400 | 90 | 82 | 20 | 27.4 | 92.60 |
| 42 | 370 | 400 | 100 | 82 | 20 | 27.4 | 92.40 |
| 43 | 370 | 300 | 80 | 82 | 20 | 18.7 | 93.20 |
| 44 | 370 | 300 | 90 | 82 | 20 | 18.7 | 94.10 |
| 45 | 370 | 300 | 100 | 82 | 20 | 18.7 | 93.40 |
| 46 | 370 | 200 | 110 | 82 | 20 | 27.4 | 91.90 |
| 47 | 370 | 400 | 90 | 82 | 20 | 19.5 | 98.30 |
| 48 | 370 | 400 | 100 | 82 | 20 | 19.5 | 98.10 |
| 49 | 200 | 100 | 90 | 37.5 | 30 | 44.4 | 89.10 |
| 50 | 200 | 200 | 90 | 37.5 | 30 | 44.4 | 88.50 |
| 51 | 200 | 400 | 90 | 37.5 | 30 | 44.4 | 89.70 |
| 52 | 200 | 600 | 90 | 37.5 | 30 | 44.4 | 89.00 |
| 53 | 200 | 800 | 90 | 37.5 | 30 | 44.4 | 87.80 |
| 54 | 200 | 1000 | 90 | 37.5 | 30 | 44.4 | 90.60 |
| 55 | 300 | 100 | 90 | 37.5 | 30 | 44.4 | 97.10 |
| 56 | 300 | 200 | 90 | 37.5 | 30 | 44.4 | 97.50 |
| 57 | 300 | 400 | 90 | 37.5 | 30 | 44.4 | 96.30 |
| 58 | 300 | 600 | 90 | 37.5 | 30 | 44.4 | 94.50 |
| 59 | 300 | 800 | 90 | 37.5 | 30 | 44.4 | 91.90 |
| 60 | 300 | 1000 | 90 | 37.5 | 30 | 44.4 | 89.00 |
| 61 | 400 | 100 | 90 | 37.5 | 30 | 44.4 | 94.30 |
| 62 | 400 | 200 | 90 | 37.5 | 30 | 44.4 | 96.10 |
| 63 | 400 | 400 | 90 | 37.5 | 30 | 44.4 | 98.10 |
| 64 | 400 | 600 | 90 | 37.5 | 30 | 44.4 | 98.70 |
| 65 | 400 | 800 | 90 | 37.5 | 30 | 44.4 | 98.20 |
| 66 | 400 | 1000 | 90 | 37.5 | 30 | 44.4 | 92.90 |
| 67 | 500 | 100 | 90 | 37.5 | 30 | 44.4 | 95.50 |
| 68 | 500 | 200 | 90 | 37.5 | 30 | 44.4 | 96.00 |
| 69 | 500 | 400 | 90 | 37.5 | 30 | 44.4 | 98.10 |
| 70 | 500 | 600 | 90 | 37.5 | 30 | 44.4 | 99.00 |
| 71 | 500 | 800 | 90 | 37.5 | 30 | 44.4 | 99.30 |
| 72 | 500 | 1000 | 90 | 37.5 | 30 | 44.4 | 92.60 |
| 73 | 350 | 50 | 120 | 100 | 30 | 42.65 | 86.50 |
| 74 | 350 | 100 | 120 | 100 | 30 | 42.65 | 87.00 |
| 75 | 350 | 150 | 120 | 100 | 30 | 42.65 | 87.00 |
| 76 | 350 | 200 | 120 | 100 | 30 | 42.65 | 87.70 |
| 77 | 350 | 300 | 120 | 100 | 30 | 42.65 | 86.20 |
| 78 | 350 | 500 | 120 | 100 | 30 | 42.65 | 87.50 |
| 79 | 350 | 700 | 120 | 100 | 30 | 42.65 | 86.00 |
| 80 | 350 | 800 | 120 | 100 | 30 | 42.65 | 86.50 |
| 81 | 300 | 50 | 120 | 100 | 30 | 42.65 | 81.50 |
| 82 | 300 | 100 | 120 | 100 | 30 | 42.65 | 84.50 |
| 83 | 300 | 150 | 120 | 100 | 30 | 42.65 | 85.20 |
| 84 | 300 | 200 | 120 | 100 | 30 | 42.65 | 84.80 |
| 85 | 300 | 300 | 120 | 100 | 30 | 42.65 | 84.10 |
| 86 | 300 | 500 | 120 | 100 | 30 | 42.65 | 83.20 |
| 87 | 200 | 50 | 120 | 100 | 30 | 42.65 | 79.90 |
| 88 | 200 | 100 | 120 | 100 | 30 | 42.65 | 79.70 |
| 89 | 200 | 200 | 120 | 100 | 30 | 42.65 | 81.50 |
| 90 | 150 | 1000 | 80 | 100 | 30 | 31.2 | 82.00 |
| 91 | 150 | 800 | 80 | 100 | 30 | 31.2 | 84.00 |
| 92 | 150 | 600 | 80 | 100 | 30 | 31.2 | 88.00 |
| 93 | 150 | 400 | 80 | 100 | 30 | 31.2 | 96.50 |
| 94 | 150 | 200 | 80 | 100 | 30 | 31.2 | 96.00 |
| 95 | 200 | 1000 | 80 | 100 | 30 | 31.2 | 86.00 |
| 96 | 200 | 600 | 80 | 100 | 30 | 31.2 | 93.00 |
| 97 | 200 | 400 | 80 | 100 | 30 | 31.2 | 98.50 |
| 98 | 200 | 200 | 80 | 100 | 30 | 31.2 | 92.00 |
| 99 | 250 | 800 | 80 | 100 | 30 | 31.2 | 92.00 |
| 100 | 250 | 600 | 80 | 100 | 30 | 31.2 | 97.00 |
| 101 | 250 | 400 | 80 | 100 | 30 | 31.2 | 97.00 |
| 102 | 300 | 1000 | 80 | 100 | 30 | 31.2 | 91.00 |
| 103 | 350 | 1000 | 80 | 100 | 30 | 31.2 | 95.50 |
| 104 | 350 | 800 | 80 | 100 | 30 | 31.2 | 98.00 |
| 105 | 350 | 600 | 80 | 100 | 30 | 31.2 | 98.00 |
| 106 | 350 | 400 | 80 | 100 | 30 | 31.2 | 95.00 |
| 107 | 600 | 300 | 50 | 100 | 50 | 28 | 98.50 |
| 108 | 700 | 300 | 50 | 100 | 50 | 28 | 99.50 |
| 109 | 800 | 300 | 25 | 100 | 50 | 28 | 95.70 |
| 110 | 800 | 300 | 40 | 100 | 50 | 28 | 95.90 |
| 111 | 800 | 300 | 75 | 100 | 50 | 28 | 96.40 |
| 112 | 800 | 300 | 100 | 100 | 50 | 28 | 96.60 |
| 113 | 800 | 300 | 120 | 100 | 50 | 28 | 96.00 |
| 114 | 800 | 600 | 50 | 100 | 50 | 28 | 98.60 |
| 115 | 800 | 900 | 50 | 100 | 50 | 28 | 98.50 |
| 116 | 800 | 1200 | 50 | 100 | 50 | 28 | 98.50 |
| 117 | 900 | 300 | 50 | 100 | 50 | 28 | 99.50 |
| 118 | 900 | 600 | 50 | 100 | 50 | 28 | 98.50 |
| 119 | 1000 | 600 | 50 | 100 | 50 | 28 | 99.50 |
| 120 | 1000 | 900 | 50 | 100 | 50 | 28 | 99.50 |
| 121 | 1000 | 1200 | 50 | 100 | 50 | 28 | 98.50 |
| 122 | 140 | 600 | 50 | 25 | 10 | 17.9 | 92.00 |
| 123 | 160 | 600 | 50 | 25 | 10 | 17.9 | 95.30 |
| 124 | 180 | 600 | 50 | 25 | 10 | 17.9 | 96.90 |
| 125 | 200 | 600 | 50 | 25 | 10 | 17.9 | 99.60 |
| 126 | 220 | 600 | 50 | 25 | 10 | 17.9 | 99.75 |
| 127 | 240 | 600 | 50 | 25 | 10 | 17.9 | 99.65 |
| 128 | 200 | 200 | 50 | 25 | 10 | 17.9 | 98.90 |
| 129 | 200 | 400 | 50 | 25 | 10 | 17.9 | 99.25 |
| 130 | 200 | 600 | 50 | 25 | 10 | 17.9 | 99.60 |
| 131 | 200 | 800 | 50 | 25 | 10 | 17.9 | 97.60 |
| 132 | 200 | 600 | 10 | 25 | 10 | 17.9 | 97.60 |
| 133 | 200 | 600 | 30 | 25 | 10 | 17.9 | 98.75 |
| 134 | 200 | 600 | 50 | 25 | 10 | 17.9 | 99.60 |
| 135 | 200 | 600 | 70 | 25 | 10 | 17.9 | 98.60 |
| 136 | 190 | 400 | 60 | 80 | 20 | 34 | 82.00 |
| 137 | 190 | 500 | 60 | 80 | 20 | 34 | 79.00 |
| 138 | 190 | 600 | 60 | 80 | 20 | 34 | 79.00 |
| 139 | 190 | 700 | 60 | 80 | 20 | 34 | 78.00 |
| 140 | 170 | 400 | 60 | 80 | 20 | 34 | 78.00 |
| 141 | 170 | 500 | 60 | 80 | 20 | 34 | 76.00 |
| 142 | 170 | 600 | 60 | 80 | 20 | 34 | 77.00 |
| 143 | 150 | 400 | 60 | 80 | 20 | 34 | 79.00 |
| 144 | 150 | 500 | 60 | 80 | 20 | 34 | 79.00 |
| 145 | 800 | 300 | 25 | 100 | 50 | 28.2 | 95.70 |
| 146 | 800 | 300 | 40 | 100 | 50 | 28.2 | 95.90 |
| 147 | 800 | 300 | 50 | 100 | 50 | 28.2 | 95.50 |
| 148 | 800 | 300 | 75 | 100 | 50 | 28.2 | 96.40 |
| 149 | 800 | 300 | 100 | 100 | 50 | 28.2 | 96.60 |
| 150 | 800 | 300 | 120 | 100 | 50 | 28.2 | 96.00 |
| 151 | 100 | 300 | 80 | 60 | 50 | 27.5 | 85.00 |
| 152 | 400 | 300 | 80 | 60 | 50 | 27.5 | 93.50 |
| 153 | 200 | 600 | 80 | 60 | 50 | 27.5 | 89.00 |
| 154 | 300 | 600 | 80 | 60 | 50 | 27.5 | 92.00 |
| 155 | 400 | 600 | 80 | 60 | 50 | 27.5 | 96.75 |
| 156 | 500 | 600 | 80 | 60 | 50 | 27.5 | 98.00 |
| 157 | 300 | 400 | 50 | 40 | 30 | 45 | 84.00 |
| 158 | 800 | 400 | 90 | 40 | 30 | 45 | 98.00 |
| 159 | 800 | 400 | 70 | 40 | 30 | 45 | 98.00 |
| 160 | 600 | 200 | 90 | 40 | 30 | 45 | 98.00 |

Source: Authors’ own work / literature research conducted by the authors

Table XIII. Random samples from table XII for the red laser validation set

| # |  |  |  |  |
| --- | --- | --- | --- | --- |
| 5 | 15 | 21 | 38 | 57 |
| 60 | 73 | 78 | 85 | 88 |
| 89 | 93 | 101 | 102 | 111 |
| 117 | 124 | 151 | 155 | 160 |

Source: Authors’ own work

Table XIV. Predictions of the relative density [%] from the PINN for the red laser validation set

| # | Output 1 | Output 2 | Output 3 | Output 4 | Output 5 |
| --- | --- | --- | --- | --- | --- |
| 1 | 86.59 | 85.50 | 86.01 | 86.91 | 88.80 |
| 2 | 95.62 | 97.40 | 96.89 | 97.01 | 96.93 |
| 3 | 88.06 | 88.49 | 85.78 | 90.34 | 86.29 |
| 4 | 94.50 | 93.97 | 94.38 | 93.89 | 94.63 |
| 5 | 98.78 | 99.07 | 98.95 | 98.62 | 97.85 |
| 6 | 82.67 | 82.73 | 82.77 | 84.38 | 84.60 |
| 7 | 85.10 | 84.68 | 84.50 | 85.60 | 87.03 |
| 8 | 99.11 | 98.68 | 98.32 | 98.99 | 98.60 |
| 9 | 84.64 | 85.77 | 85.40 | 85.70 | 87.31 |
| 10 | 95.41 | 96.51 | 96.28 | 96.52 | 96.69 |
| 11 | 90.70 | 91.04 | 90.47 | 92.85 | 91.12 |
| 12 | 94.65 | 95.20 | 95.60 | 94.79 | 94.46 |
| 13 | 95.33 | 96.29 | 96.08 | 96.40 | 96.49 |
| 14 | 82.89 | 82.57 | 82.60 | 84.44 | 84.72 |
| 15 | 96.43 | 98.10 | 97.04 | 97.52 | 97.96 |
| 16 | 94.93 | 94.39 | 95.03 | 94.85 | 94.85 |
| 17 | 95.17 | 95.94 | 95.76 | 96.25 | 96.16 |
| 18 | 94.95 | 93.95 | 95.04 | 94.78 | 94.47 |
| 19 | 90.87 | 91.41 | 88.60 | 91.67 | 91.04 |
| 20 | 97.12 | 97.51 | 97.97 | 97.09 | 96.90 |

Source: Authors’ own work

Table XV. Experimentally determined data for the green laser LPBF process

| # | Laser Power [W] | Scanning Speed [mms] | Hatch Distance [µm] | Laser Spot Diameter [µm] | Layer Thickness [µm] | Powder Size [µm] | Relative Density [%] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 190 | 1200 | 80 | 80 | 30 | 25 | 85.54 |
| 2 | 190 | 1200 | 60 | 80 | 30 | 25 | 90.01 |
| 3 | 190 | 1000 | 60 | 80 | 30 | 25 | 91.55 |
| 4 | 190 | 800 | 60 | 80 | 30 | 25 | 94.59 |
| 5 | 175 | 1000 | 80 | 80 | 30 | 25 | 88.64 |
| 6 | 175 | 1000 | 60 | 80 | 30 | 25 | 88.93 |
| 7 | 175 | 800 | 60 | 80 | 30 | 25 | 90.80 |
| 8 | 135 | 600 | 60 | 80 | 30 | 25 | 93.72 |
| 9 | 135 | 600 | 60 | 80 | 30 | 25 | 91.23 |
| 10 | 135 | 500 | 60 | 80 | 30 | 25 | 91.73 |
| 11 | 135 | 400 | 60 | 80 | 30 | 25 | 92.17 |
| 12 | 135 | 600 | 55 | 80 | 30 | 25 | 91.89 |
| 13 | 135 | 500 | 55 | 80 | 30 | 25 | 90.37 |
| 14 | 135 | 400 | 55 | 80 | 30 | 25 | 93.22 |
| 15 | 135 | 600 | 50 | 80 | 30 | 25 | 94.41 |
| 16 | 135 | 500 | 50 | 80 | 30 | 25 | 95.30 |
| 17 | 135 | 400 | 50 | 80 | 30 | 25 | 93.48 |
| 18 | 150 | 600 | 55 | 80 | 30 | 25 | 95.53 |
| 19 | 150 | 500 | 55 | 80 | 30 | 25 | 96.01 |
| 20 | 150 | 400 | 55 | 80 | 30 | 25 | 95.52 |
| 21 | 190 | 200 | 50 | 80 | 30 | 25 | 99.14 |
| 22 | 190 | 300 | 50 | 80 | 30 | 25 | 99.87 |
| 23 | 192 | 400 | 50 | 80 | 30 | 25 | 99.89 |
| 24 | 190 | 400 | 50 | 80 | 30 | 25 | 99.41 |
| 25 | 190 | 600 | 50 | 80 | 30 | 25 | 98.66 |
| 26 | 190 | 800 | 50 | 80 | 30 | 25 | 98.49 |
| 27 | 180 | 400 | 50 | 80 | 30 | 25 | 97.53 |
| 28 | 170 | 400 | 50 | 80 | 30 | 25 | 97.91 |
| 29 | 160 | 400 | 50 | 80 | 30 | 25 | 94.33 |
| 30 | 150 | 400 | 50 | 80 | 30 | 25 | 95.20 |
| 31 | 150 | 300 | 50 | 80 | 30 | 25 | 95.52 |
| 32 | 150 | 200 | 50 | 80 | 30 | 25 | 95.42 |
| 33 | 192 | 300 | 50 | 80 | 30 | 25 | 97.61 |
| 34 | 192 | 375 | 50 | 80 | 30 | 25 | 99.30 |
| 35 | 192 | 425 | 50 | 80 | 30 | 25 | 98.99 |
| 36 | 192 | 450 | 50 | 80 | 30 | 25 | 98.07 |
| 37 | 190 | 400 | 60 | 80 | 30 | 25 | 99.82 |
| 38 | 192 | 500 | 50 | 80 | 30 | 25 | 99.63 |
| 39 | 175 | 400 | 60 | 80 | 30 | 25 | 96.94 |
| 40 | 175 | 500 | 50 | 80 | 30 | 25 | 95.36 |
| 41 | 192 | 600 | 50 | 80 | 30 | 25 | 98.71 |
| 42 | 150 | 400 | 60 | 80 | 30 | 25 | 93.77 |
| 43 | 150 | 500 | 50 | 80 | 30 | 25 | 92.73 |
| 44 | 175 | 600 | 50 | 80 | 30 | 25 | 95.35 |
| 45 | 190 | 600 | 60 | 80 | 30 | 25 | 98.21 |
| 46 | 150 | 600 | 50 | 80 | 30 | 25 | 92.19 |
| 47 | 175 | 600 | 60 | 80 | 30 | 25 | 93.59 |
| 48 | 175 | 800 | 50 | 80 | 30 | 25 | 92.29 |
| 49 | 192 | 400 | 50 | 80 | 30 | 25 | 99.91 |
| 50 | 192 | 400 | 50 | 80 | 30 | 25 | 99.62 |
| 51 | 192 | 400 | 50 | 80 | 30 | 25 | 99.60 |
| 52 | 192 | 400 | 50 | 80 | 30 | 25 | 98.99 |

Source: Authors’ own work

Table XVI. Random samples from table XV for the green laser validation set

| # |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 1 | 2 | 3 | 7 | 9 | 10 |
| 11 | 24 | 28 | 38 | 43 | 52 |

Source: Authors’ own work

Table XVII. Predictions of the relative density [%] from the PINN for the green laser validation set

| # | Output 1 | Output 2 | Output 3 | Output 4 | Output 5 |
| --- | --- | --- | --- | --- | --- |
| 1 | 91.00 | 91.04 | 91.39 | 90.90 | 90.62 |
| 2 | 95.89 | 97.28 | 96.95 | 95.82 | 96.81 |
| 3 | 92.49 | 92.18 | 93.24 | 92.12 | 92.57 |
| 4 | 93.60 | 93.13 | 93.55 | 93.10 | 93.75 |
| 5 | 99.29 | 99.24 | 99.41 | 99.21 | 99.34 |
| 6 | 95.16 | 94.98 | 94.76 | 94.65 | 94.87 |
| 7 | 99.17 | 99.12 | 99.25 | 99.10 | 99.25 |
| 8 | 90.60 | 91.41 | 91.31 | 90.60 | 91.22 |
| 9 | 92.15 | 92.32 | 91.80 | 91.03 | 91.97 |
| 10 | 92.98 | 92.88 | 92.34 | 92.55 | 92.42 |
| 11 | 87.83 | 89.34 | 88.56 | 87.86 | 89.53 |
| 12 | 99.22 | 99.16 | 99.33 | 99.10 | 99.26 |

Source: Authors’ own work

NOTE: ALL FIGURES AND TABLES ARE AUTHORS’ OWN WORK