Supplementary Material

Table S1. The selected process parameters for the 316L LB-PBF process.

| Sample ID | Laser Power (W) | Scan Speed (mm/s) | Hatch Spacing (μm) | Scanning Pattern Angle (°) | Heat treatment temperature (°C) |
| --- | --- | --- | --- | --- | --- |
| 1 | 150 | 650 | 60 | 36 | 20 |
| 2 | 150 | 700 | 65 | 40 | 425 |
| 3 | 150 | 750 | 70 | 45 | 650 |
| 4 | 150 | 800 | 75 | 60 | 870 |
| 5 | 150 | 850 | 80 | 72 | 1150 |
| 6 | 175 | 650 | 65 | 45 | 870 |
| 7 | 175 | 700 | 70 | 60 | 1150 |
| 8 | 175 | 750 | 75 | 72 | 20 |
| 9 | 175 | 800 | 80 | 36 | 425 |
| 10 | 175 | 850 | 60 | 40 | 650 |
| 11 | 200 | 650 | 70 | 72 | 425 |
| 12 | 200 | 700 | 75 | 36 | 650 |
| 13 | 200 | 750 | 80 | 40 | 870 |
| 14 | 200 | 800 | 60 | 45 | 1150 |
| 15 | 200 | 850 | 65 | 60 | 20 |
| 16 | 225 | 650 | 75 | 40 | 1150 |
| 17 | 225 | 700 | 80 | 45 | 20 |
| 18 | 225 | 750 | 60 | 60 | 425 |
| 19 | 225 | 800 | 65 | 72 | 650 |
| 20 | 225 | 850 | 70 | 36 | 870 |
| 21 | 250 | 650 | 80 | 60 | 650 |
| 22 | 250 | 700 | 60 | 72 | 870 |
| 23 | 250 | 750 | 65 | 36 | 1150 |
| 24 | 250 | 800 | 70 | 40 | 20 |
| 25 | 250 | 850 | 75 | 45 | 425 |

Figure S1. The tensile curves for samples in (a) as printed state and (b) heat treated at 425 °C, (c) 650 °C, (d) 870 °C, and (e) 1150 °C temperatures. The observed numbers in the legends correspond to the test number mentioned in Table 3.

Figure S2. Variation in mechanical performance among printed samples as a function of the designed energy density range.

Table S2. The variation of the energy density with respect to the processing parameters used in this study.

| Laser Power (W) | Scan Speed (mm/s) | Hatch Spacing (µm) | Energy Density (J/mm3) |
| --- | --- | --- | --- |
| 150 | 650 | 60 | 8.82 |
| 150 | 700 | 65 | 8.19 |
| 150 | 750 | 70 | 7.64 |
| 150 | 800 | 75 | 7.17 |
| 150 | 850 | 80 | 6.74 |
| 175 | 650 | 65 | 10.29 |
| 175 | 700 | 70 | 9.55 |
| 175 | 750 | 75 | 8.92 |
| 175 | 800 | 80 | 8.36 |
| 175 | 850 | 60 | 7.87 |
| 200 | 650 | 70 | 11.76 |
| 200 | 700 | 75 | 10.92 |
| 200 | 750 | 80 | 10.19 |
| 200 | 800 | 60 | 9.55 |
| 200 | 850 | 65 | 8.99 |
| 225 | 650 | 75 | 13.23 |
| 225 | 700 | 80 | 12.28 |
| 225 | 750 | 60 | 11.46 |
| 225 | 800 | 65 | 10.75 |
| 225 | 850 | 70 | 10.12 |
| 250 | 650 | 80 | 14.70 |
| 250 | 700 | 60 | 13.65 |
| 250 | 750 | 65 | 12.74 |
| 250 | 800 | 70 | 11.94 |
| 250 | 850 | 75 | 11.24 |